Supplementary Materials for

A dislocation source efficiency-based model for grain-size-dependent ductile-to-brittle transition in tungsten

Supplemental Figures and Tables

Fig. S1 Typical temperature-dependent load-displacement curves from small punch tests for the five tungsten materials. The curves show a progressive enhancement in deformation capacity with increasing temperature. (a) RS-W, (b) BR-W, (c) UR-W, (d) FG-WK, and (e) UFG-WK.

Table S1. Estimated dislocation density parameters for the five tungsten materials investigated in this study [1,2].

| Parameters | Symbols | Value | Unit |
| --- | --- | --- | --- |
| Nucleation enthalpy pre-factor | ΔH0 | 1.63 | (eV) |
| Peierls stress | τp | 2030 | (MPa) |
| Fitting exponent | p | 0.86 | \ |
| Fitting exponent | q | 1.69 | \ |
| Critical temperature | Tc | 800 | (K) |
| Magnitude of the Burgers vector | b | 2.74×10-10 | (m) |
| Drag coefficient (screw) | Bs | 9.80×10-4 | (Pa s) |
| Boltzmann constant | kB | 1.38×10-23 | (J/K) |
| Drag coefficient (edge) | B0 | 4.26×10-4 | (Pa s) |
| Drag coefficient (edge) | B1 | 8.70×10-7 | (Pa s/K) |
| Density of dislocations generated from Frank-Read sources | ρF-R | 6.50×1014 | (m-2) |
| The characteristic length of mobile dislocations released per unit area of grain boundary | NGB | 5.00×109 | (m-1) |

Table S2. Processing history and estimated pre-existing mobile dislocation density for the five tungsten materials [3-5].

| Material | Mechanical processing history | The order-of-magnitude total dislocation density (m-2) | The fraction of mobile dislocations | Pre-existing mobile dislocations density (m-2) |
| --- | --- | --- | --- | --- |
| RS-W | Rotary swaged + annealing | ~5.00×1011 | ~60% | 3.00×1011 |
| BR-W | Bidirectionally hot rolled | ~1.00×1013 | ~80% | 8.00×1012 |
| UR-W | Unidirectionally hot rolled | ~2.00×1013 | ~80% | 1.60×1013 |
| FG-WK | Hot rolled + annealing | ~1.00×1014 | ~60% | 6.00×1013 |
| UFG-WK | Hot rolled + annealing | ~1.00×1014 | ~60% | 6.00×1013 |

* The pre-existing mobile dislocation density was calculated by multiplying the estimated order-of-magnitude total dislocation density by the appropriate fraction of mobile dislocations.

Table S3. Comprehensive dataset of microstructural and DBTT for tungsten materials compiled from the literature [3,6-12].

| Material | Average grain size-x direction (μm) | Average grain size-y direction (μm) | Average grain size-z direction (μm) | Experimental DBTT (K) |
| --- | --- | --- | --- | --- |
| HR-W (SPT) | 1.99 | 1.09 | 0.21 | 383±10 |
| REC-W (SPT) | 12.5 | 12.5 | 12.5 | 598±25 |
| RS-WK (CIT) | 105 | 5.7 | 5.7 | 573±25 |
| HR-WK (CIT) | 30 | 20 | 11 | 623±25 |
| CG-W (CIT) | 98 | 59 | 22 | 823±25 |
| CG-WK (CIT) | 111 | 55 | 55 | 923±25 |
| CR4.1-W (SENT) | 1.63 | 1.01 | 0.15 | 208±15 |
| CR3.4-W (SENT) | 1.42 | 1.10 | 0.17 | 333±15 |
| CR3.0-W (SENT) | 1.40 | 1.10 | 0.23 | 348±15 |
| CR2.5-W (SENT) | 1.46 | 1.08 | 0.26 | 358±15 |
| CR1.8-W (SENT) | 1.31 | 1.23 | 0.37 | 388±15 |
| CR-W (CIT) | 3.18 | 1.16 | 0.73 | 460±62 |
| HR-FG-W (CIT) | 8.73 | 6.46 | 3.53 | 698±50 |
| AN-W (CIT) | 21.61 | 17.53 | 11.85 | 948 |
| HR-CG-W (CIT) | 45 | 38 | 13 | 723±25 |
| CR4.1-W (SENT) | ~1.80 | ~1.11 | 0.16 | 204±31 |
| CR3.3-W (SENT) | ~1.56 | ~1.21 | 0.20 | 321±39 |
| CR2.9-W (SENT) | ~1.54 | ~1.21 | 0.24 | 354±44 |
| CR2.5-W (SENT) | ~1.60 | ~1.18 | 0.27 | 348±50 |
| CR1.7-W (SENT) | ~1.44 | ~1.35 | 0.38 | 429±44 |
| CR3.7-WK (SENT) | ~1.56 | ~1.21 | 0.16 | 208±5 |
| CR3.1-WK (SENT) | ~1.54 | ~1.35 | 0.27 | 298±5 |
| CR2.7-WK (SENT) | ~1.89 | ~1.40 | 0.34 | 323±10 |
| CR1.6-WK (SENT) | ~1.65 | ~1.55 | 0.48 | 523±10 |

* For materials where complete 3D grain size data was unavailable in the original report, missing dimensions were estimated. This estimation was guided by the material's reported thermomechanical processing history, assuming grain aspect ratios consistent with those observed in well-characterized materials subjected to similar deformation processes.

Table S4. Processing history and estimated pre-existing mobile dislocation density for selected tungsten materials from the literature [3,6,9,10].

| Material | Mechanical processing history | The order-of-magnitude total dislocation density (m-2) | The fraction of mobile dislocations | Pre-existing mobile dislocations density (m-2) |
| --- | --- | --- | --- | --- |
| HR-W (SPT) | Hot rolled + annealing | 2.70×1014 | ~60% | 1.90×1014 |
| REC-W (SPT) | Recrystallized | ~1.00×1012 | ~50% | 5.00×1011 |
| RS-WK (CIT) | Rotary swaged + annealing | ~1.00×1013 | ~60% | 6.00×1012 |
| HR-WK (CIT) | Hot rolled + annealing | ~5.00×1012 | ~60% | 3.00×1012 |
| CG-W (CIT) | Hot rolled + annealing | ~1.00×1012 | ~60% | 6.00×1011 |
| CG-WK (CIT) | Rotary swaged + annealing | ~3.00×1011 | ~60% | 1.80×1011 |
| CR4.1-W (SENT) | Cold rolled | 8.80×1014 | ~70% | 6.16×1014 |
| CR3.4-W (SENT) | Cold rolled | 9.20×1013 | ~70% | 6.44×1013 |
| CR3.0-W (SENT) | Cold rolled | 5.40×1013 | ~70% | 3.78×1013 |
| CR2.5-W (SENT) | Cold rolled | 9.90×1013 | ~70% | 6.93×1013 |
| CR1.8-W (SENT) | Cold rolled | 1.10×1014 | ~70% | 7.70×1013 |

* The pre-existing mobile dislocation density was calculated by multiplying the estimated order-of-magnitude total dislocation density by the appropriate fraction of mobile dislocations.

References

- G. Po, Y. Cui, D. Rivera, D. Cereceda, T.D. Swinburne, J. Marian, N. Ghoniem, Acta Mater. 119 (2016) 123-135.

- Y. H. Zhang, E. Ma, J. Sun, W.Z. Han, J. Mater. Sci. Technol. 141 (2023) 193-198.

- Y.H. Zhang, W.Z. Han, Acta Mater. 220 (2021) 117332.

- X.F. Xie, Z.M. Xie, R. Liu, Q.F. Fang, C.S. Liu, W.Z. Han, X. Wu, Acta Mater. 228 (2022) 117765.

- F.J. Humphreys, M. Hatherly, Recrystallization and Related Annealing Phenomena, 2nd ed., Elsevier, Oxford, 2004.

- Y.H. Zhang, E. Ma, J. Sun, W.Z. Han, Acta Mater. 264 (2024) 119586.

- J. Reiser, J. Hoffmann, U. Jäntsch, M. Klimenkov, S. Bonk, C. Bonnekoh, M. Rieth, A. Hoffmann, T. Mrotzek, Int. J. Refract. Met. Hard Mater. 54 (2016) 351-369.

- S. Nogami, S. Watanabe, J. Reiser, M. Rieth, S. Sickinger, A. Hasegawa, Fusion Eng. Des. 140 (2019) 48-61.

- C. Bonnekoh, U. Jäntsch, J. Hoffmann, H. Leiste, A. Hartmaier, D. Weygand, A. Hoffmann, J. Reiser, Int. J. Refract. Met. Hard Mater. 78 (2019) 146-163.

- S. Nogami, A. Hasegawa, M. Fukuda, M. Rieth, J. Reiser, G. Pintsuk, J. Nucl. Mater. 543 (2021) 152506.

- C. Bonnekoh, P. Lied, S. Zaefferer, U. Jäntsch, A. Hoffmann, J. Reiser, M. Rieth, Nucl. Mater. Energy 25 (2020) 100769.

- P. Lied, W. Pantleon, C. Bonnekoh, S. Bonk, A. Hoffmann, J. Reiser, M. Rieth, J. Nucl. Mater. 544 (2021) 152664.